## Slide 1
B Suitters, D Wilcox, C Densham, W Bishop, J Back
Muon Collider UK Meeting
30 April 2025
A Tungsten Target for the Muon Collider

## Slide 2: Agenda
Target Options
Motivation
Development work from previous studies
Application to the Muon Collider
Current status of target concept
Challenges
Plans

## Slide 3: Muon Production Target

## Slide 4: Target Requirements
Among the highest power on target ever proposed
Short, intense pulse
Space constraints
Power deposition on solenoids

## Slide 5: Target Options
Carbon Target (CERN, S. Candido et al.)
Liquid Lead (ENEA/CERN, C. Carelli et al.)
Fluidized Tungsten (RAL/Warwick University, this talk)

## Slide 6: Target Options
Solid Materials
Tungsten
Graphite
Beryllium
Tantalum
Simpler, known construction
Limited by thermal properties. Fragile.

## Slide 7: Target Options
Solid Materials
Tungsten
Graphite
Beryllium
Tantalum
Simpler, known construction
Limited by thermal properties. Fragile.
Liquid Materials
Mercury
Lead
Lead-Bismuth
Gallium
Power spread out across a larger volume
Cavitation, Corrosion, plant complexity

## Slide 8: Target Options
Solid Materials
Tungsten
Graphite
Beryllium
Tantalum
Simpler, known construction
Limited by thermal properties. Fragile.
Liquid Materials
Mercury
Lead
Lead-Bismuth
Gallium
Power spread out across a larger volume
Cavitation, Corrosion, plant complexity
Fluidized Powder Targets
Spreads power like liquids
Resistant to shock
No corrosion
Reliability and Erosion
Plant Complexity

## Slide 9
Peripherally cooled monolith
Flowing or rotating targets
Segmented
LHC Beam Dump Run 3, 540MJ/beam

## Slide 10
Peripherally cooled monolith
Flowing or rotating targets
Segmented
MuCol W Powder
LHC Beam Dump Run 3, 540MJ/beam
MuCol C Target
Figure For Reference Only

## Slide 11: Previous Studies
Batched process flow in air, quasi-continuous flow possible with buffer chute pressurisation
~25-250μm tungsten powder
Showed flow regimes can be manipulated with driving pressure
Active test section ~1m in length
Novel data collected for conveying tungsten powder (publication pending)

## Slide 12: Layout
Target pipe drops in from above
Heat exchangers, compressors, etc all external
Approximately 10m pipe length- determines pressure requirements

## Slide 14: Current Status
Previous work reimagined in a Muon Collider context
Rough layout devised
Feasibility of key components being assessed
  Contact made with UK academic centre
First approximations made of target heating and flow requirements
Target performance optimisation effort underway (see W Bishop)
Simulating fluidization is difficult, and hard to validate!
Gas flow in
Gas flow out
WRONG!

## Slide 15: Challenges
Heat deposition
Pressure
Erosion
Process design

## Slide 16: Heat Deposition
Intense heating on beam pulse
~5 J/mm3.pulse possible
  This must be reduced to 1.5-2 J/mm3.pulse max
Can control heating with either beam parameters or target density
Figure For Reference Only

## Slide 17: Heat Deposition
Chart: Target Diameter, mm
| 30 | 45 | 60
50% Volume Fraction, Gaussian | 1.1664 | 2.0208 | 3.1531
25% Volume Fraction, Gaussian | 1.6778 | 3.1195 | 4.6269
SuperGaussian, 25% Volume Fraction | 2.7649
Supergaussian, 50% Volume Fraction | 1.8345
Figure For Reference Only

## Slide 18: Pressure
Minimising total circuit length reduces pressure
Flow properties should scale well from previous test rig
  High, but manageable pressures ~1.5 bar/m
  Optimisation should improve this
Offline tests of each section will highlight areas of interest

## Slide 19: Erosion
University of Sheffield masters project to develop an erosion test capability
Second masters project next year to gather data
Erosion expert visiting researcher will work on this project
SiC-SiC Composite material samples on my desk ready to test!

## Slide 20: Process Design
Pneumatic conveying is a mature technology!
Only novelty is helium driving gas and high-density tungsten
UK has significant expertise in this area
  University of Greenwich Wolfson Centre
  UK Industry
Current Industrial interest in dense fluidization
  Nuclear and catalyst applications

## Slide 21: Challenges
Heat deposition
  Design in parallel with Physics optimisation
Pressure
  Minimise piping length, test with off-line rig
Erosion
  Ongoing work to assess at University of Sheffield
Process design
  Use STFC expertise in facility design
  Industrial expertise pneumatic conveying and powder handling plant
  Offline Testing!
Opportunities

## Slide 22: Summary
Fluidized Tungsten is a promising target material for higher beam powers
Focus on R&D plan
  Prioritising problem components
  Versatile, cost-efficient test rig in the future?
Increase confidence in key components through theoretical studies
Add detail to the target concept as more becomes known
Exploit opportunities for academic and industrial collaboration

## Slide 23
Questions?
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.

## Slide 24
Backup
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.

## Slide 25: Flat Topping Beam
Supergaussian Ø30mm
Allowable Beam Power 1.85MW
Gaussian Ø30mm
Allowable Beam Power 1.17MW
Allowable Power  ΔT < 600K

## Slide 26: Changing Diameter
Supergaussian Ø30mm
Allowable Beam Power 1.85MW
Gaussian Ø45mm
Allowable Beam power 2.04MW
Allowable Power  ΔT < 600K

## Slide 27: Changing Density
Supergaussian Ø30mm, 50%
Allowable Beam Power 1.85MW
Gaussian Ø30mm, 25%
Allowable Beam power 1.69MW
Allowable Power  ΔT < 600K

## Slide 28: Power on Target, Varied Parameters

## Slide 29
Chart: Beam Power vs Target Diameter
| 30 | 45 | 60
50% Volume Fraction, Gaussian | 1.1664 | 2.0208 | 3.1531
25% Volume Fraction, Gaussian | 1.6778 | 3.1195 | 4.6269
SuperGaussian, 25% Volume Fraction | 2.7649
Supergaussian, 50% Volume Fraction | 1.8345
Potential with Supergaussian?